| Product number | Type | Solid content | Recommended use | Product characteristics |
| --- | --- | --- | --- | --- |
| AC252 | Acrylic acid | 41-43% | Waxy water | Self-crosslinking, good transparency, high gloss and hardness, good grinding. |